## Slide 1
Thermophysical Properties of Fluids Importance of Accurate Data
Tecnologia Química
Valentim M.B. Nunes
April 2025

## Slide 3
Thermophysics plays an important role in the characterization of fluids.
Thermophysical properties relevant for heat transfer and heat storage applications are the density, thermal conductivity, specific heat capacity and viscosity.
The viscosity and thermal conductivity are perhaps the most important properties on the study of liquid structure, and with industrial application.
My field, High temperatures!!!

## Slide 4
Samples can react with cell walls or atmosphere giving origin to secondary reactions - purity of samples is very important
Accurate measurement of temperature is difficult
Convection and radiation contributions to heat transfer increases at high temperatures
Non-Newtonian flow can degrade results
Samples are electrically conductive

## Slide 6
H
h
r
Torsion wire
Photodetectors
He-Ne Laser
Thermocouple
Time counter
Multimeter
Cup containing molten material
Control and acquisition of data
Mirror
Furnace

## Slide 7
Systems studied so far:
Water - test of instrument – the only accepted standard for the viscosity of fluids
Molten salts - Sodium nitrate, potassium nitrate and lithium nitrate – Eutectic carbonates.
Molten alloys - Quasi eutectic Zn/Al alloys - Zn alloys with higher contents in aluminum and silicon - Al/Mg alloys.
Galinstan - Eutectic alloy of Gallium, Indium and Tin.

## Slide 8
Molten salts constitute an important class of fluids for high temperature applications, like catalytic medium for coal gasification, molten salt oxidation of wastes and latent or sensible heat storage.
Chemical Industry
Nuclear Reactors
Heat Storage/Transfer
Waste Treatment Plants
Molten Salts
In particular, molten alkali nitrates and carbonates are being used as heat transfer/storage fluids in concentrated solar power (CSP) technologies.

## Slide 9
These kind of technologies operate in ranges of temperature for which molten salts are particularly adequate, due to its main characteristics:
Liquid state in a large range of temperatures
Ability to dissolve many inorganic and organic compounds attaining high concentrations
Low vapour pressure and stability
Viscosity generally low - ions mutual independent
High heat capacity per unit volume

## Slide 10
For the proper design and performance of equipment (like pumps, pipes and heat exchanger's) it is crucial to know, with the highest accuracy possible, the properties of the fluids, in special viscosity, density, thermal conductivity and specific heat capacity. These properties strongly influences pumping costs, thereby affecting production costs.
The accuracy is affected by the use of inappropriate equipment, wrong working equations and sample impurities. For instance the size of heat transfer equipment is strongly dependent on viscosity and thermal conductivity uncertainties.

## Slide 11
High temperature alloys are very important in many industrial processes, like steelmaking, nonferrous metallurgy, aluminium smelting, foundry, glass manufacturing, among others
In fluid flow behaviour, kinetics of metallurgic process and die casting processes, viscosity and its reciprocal, fluidity, is a fundamental parameter

## Slide 12
Shell and Tubes Heat Exchanger

## Slide 13
Effect of uncertainty of thermal conductivity (in %) and viscosity (in %) on the area of a shell and tubes heat exchanger
Newton´s law of cooling:

## Slide 14
Effect of uncertainty of thermal conductivity (in %) and viscosity (in %) on the penetration distance, z, (in %) in a cold pipe [12]

## Slide 16
http://www.archimedesolarenergy.it/molten_salt.htm

## Slide 17
Chart: 1/T (K-1)
| 2.3809523809523829E-3 | 2.3255813953488385E-3 | 2.2727272727272826E-3 | 2.2222222222222279E-3 | 2.1739130434782648E-3 | 2.1276595744680851E-3 | 2.1141649048625854E-3 | 2.0833333333333394E-3 | 2.0408163265306176E-3 | 2.0283975659229339E-3 | 2.0000000000000039E-3 | 1.9607843137254923E-3 | 1.9230769230769282E-3 | 1.9047619047619093E-3 | 1.8867924528301893E-3 | 1.8518518518518558E-3 | 1.8181818181818225E-3 | 1.7857142857142865E-3 | 1.7543859649122883E-3 | 1.7452006980802803E-3 | 1.7241379310344866E-3 | 1.6949152542372913E-3 | 1.6666666666666705E-3 | 1.6393442622950826E-3 | 1.6129032258064544E-3 | 1.6051364365971133E-3 | 1.5873015873015897E-3 | 1.5625000000000033E-3 | 1.5384615384615424E-3 | 1.5151515151515184E-3 | 1.4925373134328367E-3 | 1.4858841010401201E-3 | 1.4858841010401201E-3 | 1.4705882352941181E-3 | 1.4492753623188428E-3 | 1.4285714285714307E-3 | 1.4084507042253548E-3 | 1.3888888888888935E-3 | 1.3698630136986301E-3 | 1.3513513513513542E-3 | 1.3333333333333355E-3 | 1.3157894736842129E-3 | 1.2987012987012987E-3 | 1.2936610608020706E-3 | 1.2820512820512827E-3 | 1.2658227848101273E-3 | 1.2500000000000022E-3 | 1.2345679012345707E-3 | 1.2195121951219521E-3 | 1.2048192771084338E-3 | 1.1904761904761928E-3 | 1.1764705882352979E-3 | 1.1627906976744166E-3 | 1.149425287356322E-3 | 1.145475372279496E-3 | 1.1363636363636389E-3 | 1.1235955056179781E-3 | 1.1111111111111139E-3 | 1.0989010989010996E-3 | 1.0869565217391344E-3 | 1.0752688172043E-3 | 1.06382978723404E-3 | 1.0526315789473701E-3 | 1.0416666666666673E-3 | 1.030927835051549E-3 | 1.0277492291880781E-3
Solar Salt -Nissen 1982 | 1.2946 | 1.2532 | 1.1956 | 1.1402 | 1.0872 | 1.037 | 1.0225 | 0.98975 | 0.94569 | 0.90503 | 0.86788 | 0.83435 | 0.825 | 0.825 | 0.80445 | 0.77815 | 0.75536 | 0.7359 | 0.71955 | 0.70605 | 0.69507 | 0.68625 | 0.6792 | 0.67352 | 0.67201 | 0.66877 | 0.66451 | 0.6603 | 0.65568 | 0.65017 | 0.64332 | 0.63461 | 0.62353 | 0.60951 | 0.59196 | 0.5859
Hitec - Yang et al. 2010 | 1.5205 | 1.4809 | 1.404 | 1.33 | 1.2585 | 1.1895 | 1.1693 | 1.1228 | 1.0583 | 0.9957 | 0.93502 | 0.87612 | 0.85878 | 0.81889 | 0.76324 | 0.70909 | 0.65636 | 0.60497 | 0.58981 | 0.58981 | 0.55486 | 0.50597 | 0.45823 | 0.4116 | 0.36603 | 0.32146 | 0.27786 | 0.23518 | 0.19339 | 0.15245 | 0.14033
Hitec - Gaune 1982 | 1.6818 | 1.612 | 1.5175 | 1.4903 | 1.4288 | 1.3454 | 1.2668 | 1.2292 | 1.1928 | 1.1229 | 1.0569 | 0.99444 | 0.93536 | 0.91825 | 0.87938 | 0.8263 | 0.77592 | 0.72806 | 0.68256 | 0.66935 | 0.63928 | 0.59806 | 0.55879 | 0.52134 | 0.4856 | 0.4752 | 0.4752 | 0.45148 | 0.41887 | 0.3877 | 0.35788 | 0.32933 | 0.30198 | 0.27578 | 0.25064 | 0.22653 | 0.20339 | 0.19663
Hitec - Chen et al. 2011 | 1.1891 | 1.1753 | 1.1483 | 1.1223 | 1.0972 | 1.0731 | 1.066 | 1.0497 | 1.0271 | 1.0053 | 0.98424 | 0.96383 | 0.95784 | 0.94407 | 0.92492 | 0.90637 | 0.88837 | 0.87092 | 0.86578 | 0.86578 | 0.85397 | 0.83752 | 0.82154 | 0.80601 | 0.7909 | 0.77622 | 0.76193 | 0.74802 | 0.73448 | 0.72128 | 0.71739
Hitec - Wu et al. 2012 | 0.50805 | 0.51068 | 0.51392 | 0.51662 | 0.51781 | 0.51889 | 0.52078 | 0.52237 | 0.52371 | 0.52482 | 0.52512 | 0.52576 | 0.52654 | 0.5272 | 0.52775 | 0.52822 | 0.52834 | 0.5286 | 0.52893 | 0.5292 | 0.52943 | 0.52962 | 0.52968 | 0.52968 | 0.52979 | 0.52992 | 0.53004 | 0.53013 | 0.53021 | 0.53028 | 0.53033 | 0.53038 | 0.53042 | 0.53045 | 0.53046
LiNO3 - Janz et al. 1979 | 1.6528 | 1.576 | 1.4994 | 1.4237 | 1.4013 | 1.3496 | 1.2779 | 1.2097 | 1.1461 | 1.0883 | 1.0723 | 1.0376 | 0.99529 | 0.96264
NaNO3 - Janz et al. 1979 | 1.0481 | 0.99604 | 0.94409 | 0.89247 | 0.87708 | 0.84139 | 0.79107 | 0.74177 | 0.6938 | 0.64746 | 0.63394 | 0.63394 | 0.60312 | 0.56115 | 0.52195 | 0.48592 | 0.45347 | 0.42501
KNO3 - Janz et al. 1979 | 1.0174 | 0.96252 | 0.90791 | 0.85374 | 0.80026 | 0.74777 | 0.73226 | 0.73226 | 0.69658 | 0.64706 | 0.59961 | 0.55465 | 0.51264 | 0.47406 | 0.43938 | 0.40908 | 0.38361
Solar Salt - Janz et al. 1979 | 1.5529 | 1.515 | 1.4773 | 1.4021 | 1.3277 | 1.2543 | 1.1823 | 1.161 | 1.1119 | 1.0435 | 0.97735 | 0.91389 | 0.85337 | 0.83583 | 0.79606 | 0.74216 | 0.69181 | 0.64508 | 0.60193 | 0.58967 | 0.58967 | 0.56223 | 0.52573 | 0.4921 | 0.46088 | 0.43155
KNO3 - Abe et al. 1980 | 1.001 | 0.96251 | 0.90902 | 0.85719 | 0.80692 | 0.75816 | 0.74381 | 0.74381 | 0.71083 | 0.66487 | 0.62023 | 0.57684 | 0.53466 | 0.49363 | 0.45371 | 0.41486 | 0.37703 | 0.34018 | 0.32931 | 0.30428 | 0.26928 | 0.23516 | 0.20188 | 0.16942 | 0.13774 | 0.10681 | 0.076605 | 0.047106 | 0.018286 | 0.0097683 | -0.0098799 | -0.037413 | -0.064333 | -0.090663 | -0.11642 | -0.14162 | -0.16629 | -0.19044 | -0.21408 | -0.23724
KNO3 - Schardey et al. 1988 | 0.98189 | 0.96623 | 0.93025 | 0.88023 | 0.83174 | 0.78473 | 0.73911 | 0.7257 | 0.7257 | 0.69484 | 0.65186 | 0.6101 | 0.56951 | 0.53006
KNO3 - Tolbaru et al. 1998 | 0.74881 | 0.73409 | 0.73409 | 0.70026 | 0.65311 | 0.60732 | 0.56281 | 0.51955 | 0.47746 | 0.43652
?
?

## Slide 18
Chart: T/K
| 380 | 390 | 400 | 410 | 420 | 426 | 430 | 440 | 450 | 460 | 470 | 480 | 490 | 500 | 510 | 520 | 530 | 540 | 550 | 560 | 570 | 580 | 590 | 600 | 610 | 620 | 630 | 640 | 650 | 660 | 663 | 670 | 673 | 680 | 690 | 700 | 710 | 720 | 730 | 740 | 750 | 760 | 770 | 776 | 780 | 790 | 800 | 810 | 820 | 830 | 840 | 850 | 860 | 870 | 873
Hitec - Janz et al. 1981 | 2505.2642 | 2486.7264 | 2441.3957 | 2397.5133 | 2355.0791 | 2314.0932 | 2274.5555 | 2236.4661 | 2199.825 | 2164.6321 | 2130.8875 | 2098.5912 | 2067.7431 | 2038.3432 | 2010.3917 | 1983.8884 | 1958.8333 | 1935.2265 | 1913.068 | 1892.3577 | 1873.0957 | 1855.282 | 1838.9165 | 1823.9993 | 1810.5303 | 1806.772 | 1798.5096 | 1795.1858 | 1787.9371 | 1778.8129 | 1771.137 | 1764.9093 | 1760.1299 | 1756.7988 | 1754.9159 | 1754.4812 | 1755.4949 | 1757.9568 | 1760.1291
Solar Salt - Zavoico 2001 | 1494.0582 | 1495.7782 | 1497.4982 | 1499.2182 | 1500.9382 | 1502.6582 | 1504.3782 | 1506.0982 | 1507.8182 | 1509.5382 | 1510.0542 | 1511.2582 | 1511.7742 | 1512.9782 | 1514.6982 | 1516.4182 | 1518.1382 | 1519.8582 | 1521.5782 | 1523.2982 | 1525.0182 | 1526.7382 | 1528.4582 | 1529.4902 | 1530.1782 | 1531.8982 | 1533.6182 | 1535.3382 | 1537.0582 | 1538.7782 | 1540.4982 | 1542.2182 | 1543.9382 | 1545.6582 | 1546.1742
Hitec - Boerema et al. 2012 | 1413.15 | 1407.15 | 1403.15 | 1393.15 | 1383.15 | 1373.15 | 1363.15 | 1353.15 | 1343.15 | 1333.15 | 1323.15 | 1313.15 | 1303.15 | 1293.15 | 1283.15 | 1273.15 | 1263.15 | 1253.15 | 1243.15 | 1233.15 | 1223.15 | 1213.15 | 1203.15 | 1193.15 | 1183.15 | 1173.15 | 1170.15 | 1163.15 | 1160.15 | 1153.15 | 1143.15 | 1133.15 | 1123.15 | 1113.15 | 1103.15 | 1093.15 | 1083.15 | 1073.15 | 1063.15 | 1057.15 | 1053.15 | 1043.15 | 1033.15 | 1023.15
LiNO3 - Janz et al. 1979 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542 | 1614.6542
NaNO3 - Janz et al. 1979 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813 | 1825.7813
KNO3 - Janz et al. 1979 | 1340.9991 | 1340.9991 | 1340.9991 | 1340.9991 | 1340.9991 | 1340.9991 | 1340.9991
Solar Salt - Janz et al. 1979 | 1748.268 | 1736.7342 | 1725.2004 | 1713.6666 | 1702.1328 | 1690.599 | 1679.0652 | 1667.5314 | 1655.9976 | 1644.4638 | 1632.93 | 1621.3962 | 1609.8623 | 1598.3285
LiNO3 - Takahashi et al. 1988 | 2060 | 2060 | 2060 | 2060 | 2060 | 2060 | 2060 | 2060 | 2060 | 2060 | 2060 | 2060
NaNO3 - Takahashi et al. 1988 | 1670 | 1670 | 1670 | 1670 | 1670 | 1670 | 1670
KNO3 - Takahashi et al. 1988 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390 | 1390
Quaternary - Wang et al. 2013 | 1384.736 | 1391.808 | 1398.88 | 1405.952 | 1413.024 | 1417.2672 | 1420.096 | 1427.168 | 1434.24 | 1441.312 | 1448.384 | 1455.456 | 1462.528 | 1469.6 | 1476.672 | 1483.744 | 1490.816 | 1497.888 | 1504.96 | 1512.032 | 1519.104 | 1526.176 | 1533.248 | 1540.32 | 1547.392 | 1554.464
Quaternary - Fernandez et al. 2015 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518 | 1518
Hitec

## Slide 19
Chart: T/K
| 497.5 | 509.4 | 530 | 545.29999999999995 | 549 | 553 | 558 | 571 | 573.70000000000005 | 587 | 590 | 592.20000000000005 | 602 | 610 | 616 | 625 | 632 | 644 | 652 | 657 | 663 | 666 | 673 | 673 | 680 | 690 | 695 | 700 | 710 | 720 | 730 | 740 | 750 | 760 | 770 | 773 | 780 | 790 | 800 | 810 | 820 | 830 | 840 | 850 | 860 | 870 | 873
Solar Salt - Janz et al. 1979 | 0.50727 | 0.50842 | 0.5115 | 0.51535 | 0.51805 | 0.51939 | 0.51939 | 0.52074 | 0.52267 | 0.52363 | 0.52459 | 0.52651 | 0.52844 | 0.53036
Hitec - Wu et al. 2012 | 0.39528 | 0.39355 | 0.38504 | 0.38312 | 0.38171 | 0.37544 | 0.37032 | 0.36648 | 0.36072 | 0.35624 | 0.34856 | 0.34344 | 0.34024 | 0.3364 | 0.33448 | 0.33 | 0.33 | 0.32552 | 0.31912 | 0.31592 | 0.31272 | 0.30632 | 0.29992 | 0.29352 | 0.28712 | 0.28072 | 0.27432 | 0.26792 | 0.266
Hitec - Yang et al. 2010 | 0.41055 | 0.40794 | 0.40468 | 0.39619 | 0.39442 | 0.38574 | 0.38378 | 0.38234 | 0.37594 | 0.37072 | 0.3668 | 0.36092 | 0.35635 | 0.34852 | 0.34329 | 0.34003 | 0.33611 | 0.33415 | 0.32958 | 0.32958 | 0.32501 | 0.31848 | 0.31521 | 0.31195 | 0.30542 | 0.29889 | 0.29236 | 0.28583 | 0.2793 | 0.27277 | 0.26624 | 0.26428
Solar Salt - Zavoico 2001 | 0.49959 | 0.5001 | 0.50263 | 0.5032 | 0.50362 | 0.50548 | 0.507 | 0.50814 | 0.50985 | 0.51118 | 0.51346 | 0.51498 | 0.51593 | 0.51707 | 0.51764 | 0.51897 | 0.51897 | 0.5203 | 0.5222 | 0.52315 | 0.5241 | 0.526 | 0.5279 | 0.5298 | 0.5317 | 0.5336 | 0.5355 | 0.5374 | 0.53797 | 0.5393 | 0.5412 | 0.5431 | 0.545 | 0.5469 | 0.5488 | 0.5507 | 0.5526 | 0.5545 | 0.5564 | 0.55697
LiNO3 - Janz et al. 1979 | 0.61024 | 0.61344 | 0.61421 | 0.61505 | 0.61609 | 0.61881 | 0.61938 | 0.62216 | 0.62279 | 0.62325 | 0.6253 | 0.62697 | 0.62823 | 0.63011 | 0.63157 | 0.63409 | 0.63576 | 0.6368 | 0.63806 | 0.63869 | 0.64015 | 0.64015 | 0.64162 | 0.64371 | 0.64475 | 0.6458 | 0.64789 | 0.64998 | 0.65208
NaNO3 - Janz et al. 1979 | 0.56071 | 0.56128 | 0.56386 | 0.56596 | 0.56754 | 0.5699 | 0.57174 | 0.57489 | 0.577 | 0.57831 | 0.57989 | 0.58068 | 0.58251 | 0.58251 | 0.58435 | 0.58698 | 0.5883 | 0.58961 | 0.59224 | 0.59486 | 0.59749 | 0.60012
KNO3 - Janz et al. 1979 | 0.45907 | 0.46125 | 0.46453 | 0.46708 | 0.47144 | 0.47436 | 0.47618 | 0.47836 | 0.47945 | 0.482 | 0.482 | 0.48455 | 0.48819 | 0.49001 | 0.49183 | 0.49547 | 0.49911 | 0.50275
Solar Salt - Omotani et al. 1982 | 0.4539 | 0.45152 | 0.4474 | 0.44434 | 0.4436 | 0.4428 | 0.4418 | 0.4392 | 0.43866 | 0.436 | 0.4354 | 0.43496
NaNO3 - Nagasaka et al. 1991 | 0.51464 | 0.5141 | 0.5137 | 0.51194 | 0.5105 | 0.50942 | 0.5078 | 0.50654 | 0.50438 | 0.50294 | 0.50204 | 0.50096
KNO3 - Nagasaka et al. 1991 | 0.40875 | 0.4063 | 0.4021 | 0.3993 | 0.39755 | 0.39545 | 0.3944 | 0.39195 | 0.39195 | 0.3895 | 0.386 | 0.38425 | 0.3825 | 0.379
KNO3

## Slide 20
Pipes
Heat Exchangers

## Slide 21
21

## Slide 23
https://webbook.nist.gov/chemistry/fluid